## Slide 1: CCM-86: Low Mass Plastic CEPS Housing
Description
  A low mass plastic CEPS housing to replace aluminum housings
Motivation: 7.5
Deliverables
  Development of material, geometry and processing
  Evaluate prototype performance and durability
Timing
  May 2015 – AM bottoming results
  July 2015 – Received 25 more housings
  August 2015 – Impact Testing
Team Members/Customers
  Team: Brandon King, Jason Rutkiewicz, Nick Mehl,
  Brian Magnus
  Customers: Pursuits Team
Last updated: July 14, 2015

## Slide 2: CCM-86: Low Mass Plastic CEPS Housing
Status Update:
First tuning loop parts being dimensionally evaluated and tested
  CMM of all critical dimensions
  Thermal cycling with backdrive evaluations at each stage
  Thermal cycling with CMM of critical dimensions
  Completed 1 life of Haitec 60 Nm bottoming
    Noticed free play in worm axis
      Bearing bore on the motor side too large. Will be addressed in next tuning loop
Material being evaluated by Casey Bentoski in METlab
Challenges:
Tuning dimensions to tolerance
Functional measurement plan
Thermal stability of parts
Creep stability of parts
Cost savings to Aluminum
Last updated: July 14, 2015
Next Actions:
Impact testing
AM friction vs temperature
NVH
Tuning the molds
Supplier - insert retention testing