## Slide 1: CCM-87: Short T-bar No Profile Grind (Gen 5)
Description
  No profile grind short t-bar, shallower holes, shorter stop tooth travel, increased hardness, larger press interference range, higher press load tolerance & lower hysteresis
Motivation : 7.0
Deliverables
  Lower hysteresis and cost
  Press & fatigue robustness
  MQ, PV Build success
    Capable to +/- 1° stop tooth balance
Timing
  Now, Fiasa and BMPV
Team Members/Customers
  Team names: Dan Diffin
  Customers: Applications Teams
Last updated: 01JA15
Gen 3
Gen 5

## Slide 2
Status Update:
$0.39 savings over Gen 3
Hysteresis below 0.2Nm
Robust to press & short stop tooth fatigue
  Can not open up short stop tooth travel due to fatigue sensitivity due to spline root sub the active section dia.
Many changes to the rolling machine and process parameters has improved serration OD size and roundness but did not improve balance
Last updated: 08JN15
CCM-87: Short T-bar No Profile Grind (Gen 5)
Challenges:
Stop tooth balance capability
  Latest bars made for Faisa MQ2 (263 asms)
    Need to be capable to +/-1°
    +/- 1° ppk: 0.58
    +/- 2° ppk: 1.10
Min torque before stop tooth contact below 8Nm requirement
Next Actions:
250 part trial for BMPV
Alternative/extra processes
    End feed rolling: Promising results but no production machine available
  Coining to form end of serration post rolling