## Slide 1: FE142: LOW COST SMALL DIAMETER TORQUE SENSOR
Comparison of proposed designs with production design
Picture |  |  |  |  | 
Design type | Axial ring magnet | SPM radial magnet | Spoke IPM- Ferrite | Spoke IPM-SmFeN | IPM Production
Linear gain | 25.6 Gauss/deg | 26.06 Gauss/deg | 28.17 Gauss/deg | 27.22 Gauss/deg | 25 Gauss/deg
Outermost diameter | 47.06mm | 51.88mm | 55.3mm | 49.36mm | 51.88mm
Permanent magnet strength | Br = 0.73T | Br=1.2T | Br=0.38T | Br=0.76T | Br=1.2T
PM material | Injection molded SmFeN | Sintered NdFeB (same as production) | Sintered Ferrite | injection molded SmFeN | Sintered NdFeB
Total permanent magnet volume | 1250.8 mm3 | 829.44mm3 | 5607 mm3 | 1260mm3 | 1305mm3
PM density | 6.2g/cc | 7.57g/cc | 5g/cc | 6.2g/cc | 7.57g/cc
Cost of PM (p.u of prod. NdFeB) | 0.6165 | 0.64 | 0.2148 | 0.6214 | 1
Pros (w.r.t production small diameter design) | Smaller diameter, lower PM cost, less steel material in lower rotor and upper rotor | Less PM material (reduction by 36.44%) Keeps prod. stator | Least and stable PM cost, less steel material in lower rotor | Lower PM cost, smaller diameter, less steel material in lower rotor | baseline
Cons(w.r.t production) | Injection molding with axially placed iron ring | same as prod. (i.e. dependency on rare-earth magnet) | Larger diameter, magnetizing fixture to magnetize spoke pattern | Magnetizing fixture to magnetize spoke pattern | Baseline

## Slide 2: FE142: LOW COST SMALL DIAMETER TORQUE SENSOR
Proposed design- Spoke IPM with Ferrite magnets
3D view of the entire magnet assembly (7 pole pair)
Si-steel / Carbon steel lamination
Magnet(ferrite, 0.38T)
Carbon steel shaft
For upper and lower rotor laminations – LH Industry
For Ferrite magnets – Bomatec
Effect of temperature on sensor gain: shown in Table I.
Effect of temperature on demagnetization: magnets not prone to demagnetization at low and high temperature
Si-steel plates
Temperature | 20oC | 140oC | -40oC
Gain [gauss/deg] | 28.17 | 20 | 32.84
Table I